**PROFILE**

* Established in 1998, **AANGEE**is a global leader in developing and manufacturing very high quality **PIGMENTS AND MONO CONCENTRATES**for the plastics industry.
* All products are of the highest quality and standards, and are developed with the customer in mind, guaranteeing flexibility, versatility and efficiency at all times.
* For last many years we are growing exponentially due to new applications and state of the art quality system
* We are exporting to many countries in the world

**APPLICATIONS**

AANGEE MANUFACTURES PIGMENTS ,MONO CONCENTRATES FOR

* MASTERBATCH INDUSTRIES
* MONO AND MULTI FILAMENT YARN AND ROPES
* PP AND POLYESTER YARN
* NON WOVEN
* LAMINATIONS
* **PRODUCTS**

PIGMENTS-

ORGANIC PIGMENTS

IN ORGANIC PIGMENTS

HIGH PERFORMANCE PIGMENT

IRON OXIDES

SOLVENT DYES

COLOUR CONCENTRATE(SINGLE PIGMENT CONCENTRATES)

ORGANIC PIGMENTS

INORGANIC PIGMENTS

HIGH PERFORMANCE PIGMENT

IRON OXIDES

SOLVENT DYES

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| GRADE | CODE | PIGMENT | %OF ACTIVE CONTENT | CARRIER RESIN | FPV (10 MICRON) |
| ANG-YELLOW 13 | PC2001 | YELLOW 13 | 40 | PP | <1 |
| ANG-YELLOW 17 | PC2002 | YELLOW 17 | 40 | PP | <1 |
| ANG-YELLOW 138 | PC2003 | YELLOW 138 | 40 | PP | <1 |
| ANG-ORANGE 13 | PC2004 | ORANGE 13 | 40 | PP | <1 |
| ANG-ORANGE 34 | PC2005 | ORANGE 34 | 40 | pp | <1 |
| ANG-RED 48:2 | PC2006 | RED 48:2 | 40 | PP | <1 |
| ANG-RED 48:3 | PC2007 | RED 48:3 | 40 | PP | <1 |
| ANG-RED 53:1 | PC2008 | RED 53:1 | 40 | PP | <1 |
| ANG-RED 57:1 | PC2009 | RED 57:1 | 40 | pp | <1 |
| ANG-RED 254 | PC2010 | RED 254 | 40 | PP | <1 |
| ANG-GREEEN 7 | PC2020 | GREEEN 7 | 40 | PP | <1 |
| ANG-BLUE 15:1 | PC2030 | BLUE 15:1 | 40 | PP | <1 |
| ANG-BLUE 15:3 | PC2040 | BLUE 15:3 | 40 | PP | <1 |
| ANG-VIOLET 23 | PC2050 | VIOLET 23 | 30 | PP | <1 |
| ANG-VIOLET 19 | PC2060 | VIOLET 19 | 30 | PP | <1 |
| ANG-RED 122 | PC2070 | RED 122 | 30 | pp | <1 |
| ANG-ORANGE 64 | PC2080 | ORANGE 64 | 30 | PP | <1 |